328	5

TRANSISTORS ● POWER SWITCH
––––––––––––––––––––––––––––––––––––––––––––––––––––––––––––––––––––––––
KU 611, KU 612 NPN – FOR SWITCHING AND REGULATORY APPLICATIONS
NPN – TPAHЗИCTOP ДЛЯ ПEPEKЛЮЧAЮЩИX И УПPABЛЯЮЩИX CXEM ● NPN – TRANSISTOR FOR SWITCHING AND CONTROL CIRCUITS ● NPN TRANSISTOREN FÜR SCHALTVORGÄNGE UND REGULATION
10 W Silicon switching power transistors, manufactured using MESA-epitaxy technology, intended for use in switching and various regulation circuits with a current of up to 10 A.
Metal case with two glass isolated passages for base and emitter.
The collector is conductively connected to the housing.
Weight: max. 12 g.
• For sockets covered with	solder, max. 1,3 mm.
•• It is measured at a distance	of max. 1,5 mm od pouzdra.
Absolute max limits:	Tc = +25 °C
			KU 611	KU 612

Collector-base voltage	UCBO	max.	210	250	V
Collector-emitter voltage (RBE = ∞)	UCEO	max.	50	80	V
Emitter – Base Voltage	UEBO	max.	3		V
Collector current	IC	max.	3		A
Emitter current	– IE	max.	3,5		A
Base current	IB	max.	0,5		A
Power dissipation UCE ≤ 20 V, Tc ≤ 45 °C	Ptot	max.	10		W
Junction temperature	Tj	max.	+155		°C
Storage temperature	Tstg	max.	–50 ... +50		°C
Internal thermal resistance (UCE ≤ 20 V)	Rthjc		≤11		K/W

Charakteristické údaje:	Tc = +25 °C
Jmenovité hodnoty:		KU 611	KU 612
* Collector voltage
(IC = 0,2 A) 1) KU 611	UCEO	≥50	–	V
(IC = 0,2 A) 1) KU 612	UCEO	–	≥80	V
* Collector-base residual current
(UCB = 30 V)	ICBO	1 ≤ 50	0,5 ≤ 50	µA
Collector-emitter residual current
(UCE = 60 V, RBE = 30 Ω) KU 611	ICER	≤300	–	µA
(UCE = 120 V, RBE = 30 Ω) KU 612	ICER	–	≤300	µA
Collector-base residual current
(UEB = 3 V)	IEBO	≤3	≤3	mA
* Collector saturation voltage
(IC = 1 A, IB = 0,1 A)	UCE sat	0,16 ≤ 1	0,16 ≤ 1	V

1) Measured in pulses, pulse width tp = 100 µs, repetition frequency tp = 50 Hz.

Note: This translation is based on a direct transcript of the original Czech datasheet. Shown on the next pages are this original datasheet and the initial transcript. Note that the sole purpose of the transcript is to ease any future translation efforts. This transcript and translation does not imply any IP-rights on my behalf, I’ve not done any more that actually transcribe and translate the original document, recreating some graphical elements in the process. So, nothing much really.
Cheers!
Gjermund Skogstad
Norway